## Slide 1: 기계학습 포텐셜 기반 촉매 연구 체험하기
구근호 켄텍 조교수

## Slide 2: Limitations of Theoretical Simulations
Molecular Dynamics
Local equilibrium
Ideal structures
time scale
length scale
Density functional theory
Limitations
Phenomenological kinetics
Pre-defined lattice and reactions
Kinetic Monte Carlo
Lack of spatial resolution
Multi Scale Simulation Methods

## Slide 3: Machine Learning Potential
Density functional theory
Force field
Machine learning potential
Adequately accurate, but slow
Fast but not as accurate
E
F
Potential Energy Surface
As accurate as the data and fast, but building data set takes time
Simulation Methods

## Slide 4: Large DFT Databases
Ulissi and coworkers. ACS Catal. 2021, 11, 6059; ACS Catal. 2023, 13, 3066
Open Catalyst 2020
~264 million DFT data points
(Transition metal catalysts)
Open Catalyst 2022
~10 million DFT data points
(Transition metal oxide catalysts)
Materials Project Trajectory
~50 million DFT data points
(Crystals)

## Slide 5: Universal Machine Learning Potential
ChgNet trained on millions of crystal data
Nat. Mach. Intell. 2023, 5, 1031
Gemnet-oc trained on millions of adsorbate and surface data
ACS Catal. 2023, 13, 5, 3066
Universally applicable for various materials
Open catalyst Database
The Materials Project
Database
Energy MAE = 0.233 eV
Force MAE = 0.021 eV/Å
Energy MAE = 0.03 eV/atom
Force MAE = 0.077 eV/Å

## Slide 6: Large Scale Simulation with Machine Learning Potential
Application
DFT speed up
Long time MD simulation
Faster catalyst screening
Larger scale catalyst mechanism research
  Interface
  Coverage effect
  Surface reconstruction
Phonon calculations
  Superconductivity
  Ionic conductivity
  Ferroelectric search
Deng et al. Nature Machine Intelligence, 2023, 5, 1031
Phase transition simulation of o-Li0.5MnO2 to s-Li0.5MnO2

## Slide 7: Jagged Pt Nanowire has High Specific HER Activity
1Duan and coworkers, Science, 2016, 354, 1414 2Duan and coworkers, Nature Catal. 2019, 2, 495
Chart: 
 | 0.81698 | 7.0507
Jagged Pt nanowire increase activity1
Pt/C
PtNW2
Ni dealloyed from NiPt straight nanowire
J [A/mgPt]
HER
~18,000 unique binding sites
10 years worth of DFT calculations
DFT-based investigation cannot be used
2H+ + 2e- → H2(g)
>5x

## Slide 8: Fully Multiscale Phenomenon Simulation
H2+OH-
H2O+e-
Heyrovsky
Pt
Pt
H
H2O+e-
Volmer
Pt
H
H
Volmer
H2
Tafel
OH-
H2O+e-
OH-
Density Functional Theory
Build ML database
BEP relations
Force Field
Molecular Dynamics
Synthesize nanowire and slab
Deep Learning
Predict adsorption energy
Mechanistic
Insights
Structure Motifs
Kinetic Monte Carlo
TOF, mechanism
Model Validation
BEP Relations
Cluster Expansion
E
102 nm, 103 ps
100 nm, 10-6 ps
102 nm, 10-6 ps
100 nm, 10-6 ps
102 nm, 10-6 ps
102 nm, 1012 ps
Human Time, length
Labeled Site
Gu et al. J. Am. Chem. Soc. 2021, 143, 5355

## Slide 9: Kinetic Monte Carlo Simulation
Top site
Bridge site
Hollow site
Occupied by H
Unoccupied
H diffusion
H+ adsorption
H2 gas formation
Initialize
Select Process
Update Graph
Increment Time
End
Start
End Time?
Yes
No
KMC Flow Chart
Gu et al. J. Am. Chem. Soc. 2021, 143, 5355

## Slide 10: Reproducing the DFT Result with MLP
NH3 -> NH2 + H
NH2 -> NH + H
NH -> N + H
on Metal Catalyst

## Slide 11: Energy Calculations

## Slide 12: Machine Learning Model

## Slide 13: Install Instruction
https://github.com/GuGroup/ocp-practice-gu
Download and install miniforge https://github.com/conda-forge/miniforge/releases/ (Miniforge3-24.11.0-1-Windows-x86_64.exe)
Download CatEnv.yml
Click search and open "Miniforge Prompt"
Go to the path of CatEnv.yml by using cd command
Type and enter "mamba env create -f CatEnv.yml"
Follow the instruction and you are all set!

## Slide 14: Reproducing the Result
What MLP calculates
What the paper calculated

## Slide 15: Reproducing the Relative Energy
As MLP will give energy of
The MLP calculation of H* and HyN* gives the energy of:
(1)
(2)
If we have energy for:
(3)
Then we can calculate the paper’s result of
(rel)
by
3E(1)+E(2)+E(3) = Erel
I calculated E(3) for you (1.0763 eV)

## Slide 16: Reproducing the Reaction Energy
(1)
(2)
E(1)+E(2)= Erxn